## Slide 1: L6: Diffraction I
Nami Matsubara
KTH Royal Institute of Technology
namim@kth.se

## Slide 2: Outline
Neutrons vs x-rays
Instrumentation
Powder and single crystal diffraction
The Rietveld method
Total scattering
Magnetic diffraction
Notes: I think you all downroad Fullprof.

## Slide 3: 6 Blind men and the elephant
X-ray
Neutron
Modeling
FTIR
Raman
Electron
Notes: It is a story of a group of blind men, who have never meet with an elephant before and who learn what the elephant is like by touching it. Each blind man feels a different part of the elephant's body, but only one part. They then describe the elephant based on their limited experience and their descriptions of the elephant are different from each other.
We can apply same story to the material science,
In our case, elephant is c onsidered material. Each blind men could be each technique. They all have different eyes thus it is very important to combine together to understand your material deeply.

## Slide 4: Different eyes: X-ray vs Neutron
6 Electrons
6 Neutrons + 6 Protons
Carbon atom C6
Notes: Here is a carbon atom, and comprises of nucleas and electrons

## Slide 5: Different eyes: X-ray vs Neutron
6Electrons
6 Neutrons + 6 Protons
Carbon atom C6
X-ray
X-ray
X-ray has interactions with the electrons.
X-rays are scattered by electron cloud of atoms.
Form factor of X-ray has atomic number dependence.
Small penetration depth
Surface studies
Notes: X-ray has interaction with these electrons,
The scattered wave from an atom is proportional to the atomic number.

## Slide 6: Different eyes: X-ray vs Neutron
6 Electrons
6Neutron + 6Proton
Carbon atom C6
Neutron (Structure )
Neutron
Neutrons are uncharged and has interactions with the the nuclei.
Neutrons are scattered by nuclei (point).
Scattering length of neutron is random.
Deep penetration depth
Large volume of sample
Bulk studies of samples
Notes: On the other hand neutron has intraction with nucles.

## Slide 7: Scattering length
Periodic table with scattering length
Isotope dependence
Light atoms
Different contrast with X-ray
Isotope dependence
Bacon, Neutron diffraction
Notes: The radii of the circles are propoftional to scattering length.
The variation of scattering amplitude is in general a slight increase with Z number.
But it is still considered as irregular.
As you can see, most atoms scatter neutrons also equally well, in contrast to the rapid increase with atomic number of the X-ray scattering amplitude.
Unlikely X-ray, it also has isotope dependence. For example, hydrogen and ditulium,

## Slide 8: High penetration
Many different sample environments!
Low temperature
Magnetic field
High pressure
High temperature
Notes: Due tot the high penetration depth, we can actually set up various sample enviroment for neutron experimment.

## Slide 9: Different eyes: X-ray vs Neutron
Neutron (Spin)
Neutron
Neutrons are uncharged but do have a magnetic moment (Spin 1/2).
An additional scattering due to the dipole-dipole interaction between the nuclear spin of neutron and the unpaired electrons (outer shell).
N
Notes: The nuclear spin of the neutron undergoes a dipole dipole interaction with the unparied electrons in the magnetic material.
Thus when the spins are ordered, magnetic Bragg peaks will emarge.

## Slide 10: Form factor
X-ray
F(Q)
Q
X-ray
Neutrons
Neutrons
F(Q)
Q
Nuclear
F(Q)
Q
Spin
Notes: As the angle between the incident and scattered directions increases, this amplitude will fall off quite rapidly
On the other hand, neutron shows no variation with the angle theta. This different comes from the fact that the dimensions of the electronic cloud are comparable with the wavelength of the X-rays whereas neutron scatters by point.

## Slide 11: How different?: Example:Mn0.3Fe0.7
Mn0.3Fe0.7
 | Fe | Mn
Neutron | 9.45 | -3.73
X-ray (Z- number) | 26 | 25
More information at high-Q
The profile is simpler
The different scattering contrast among the elements
Simulated pattern
X-ray
Neutron

## Slide 12: How different?: Example:BiMnTeO6
BiMnTeO6
 | Bi | Mn | Te | O
Neutron | 8.532 | -3.73 | 5.8 | 5.8
X-ray (Z- number) | 83 | 25 | 52 | 6
D2B, ILL
BL04, ALBA
More information at high-Q
The profile is simpler
The different scattering contrast among the elements
Notes: - the weight of the different atoms is more equilibrated
-determination of the structural parameters possible

## Slide 13: Neutron vs X-ray: Practical
X-ray
  Daily used to provide structural information on compounds, identify samples and check the quality of sample
  Both powder and single crystal, Both inhouse and synchrotron
Neutron diffraction
  Combining with X-ray, it is good complimentary techniques to determine crystal structure
  Also possible to see magnetic ordering
  Need to be performed at large scale facilities
  Required large volume of samples (powder and single crystal)
Notes: Non destructive

## Slide 14: Before… Writing the proposal
Good sample – single phase, good crystallinity
Basic characterization
  XRD in the laboratory
  Crystal structure
  Chemical compositions
  Physical properties
Choose best techniques and beamline
  What do you want to know from the diffractions????
Notes: Indexing_powder_diffraction_data_TCH.pdf

## Slide 15: Current sources
Main reactors in Europe
ILL – Grenoble
FRM II – Munich
Orphee-LLB – Saclay (end ~ 2020)
BERII-HZB (end ~ 2020)
BNC – Budapest
IRI – Delft
Gatchina – Russia
NPL – Prague
Spallation sources in the world
SNS – Oakridge
J-PARK – Japan
C-SNS – China
ISIS – Oxford
LANSCE – USA
SINQ-PSI – Switzerland
ESS – Lund

## Slide 16: Neutron source
Reactor : Continues
  High energy is rather difficult
  High average flux
Spallation: Pulsed
  High energy is good but low energy is difficult
  Very high flux in pulse, but rather low average flux
  Diffraction: T.O.F method
https://europeanspallationsource.se

## Slide 17: Constant wavelength v.s. TOF
Constant wavelength
  Higher Flux
  Monochomater (resolution)
ILL
D1A, D1B, D2B, D9, D10, D19, D20, …
LLB
3T2, G4.1, G4.2, 5C1, 5C2, 6T2 …
FRMII
SPODI, BIODIFF, RESI, HEiDi …
Time of Flight
  Wide Q-range (many detector banks)
  Pulse-source (Moderator)
ISIS
GEM, WISH, POLARIS, HRPD, HiPr, SXD …
SNS
POWGEN, SINGLE CRYSTAL, POWDER, SNAP, TOPAZ …
J-PARC
iMATERIA, SPICA, superHRPD, iBIX, SENJU
ESS
  DREAM, MAGiC
Single crystal
Notes: https://slideplayer.com/slide/12965639/

## Slide 18: Different techniques
DIffraction
Neutron
Spallation source
T.O.F
Continuous source
X-ray
Monochromatic beam
Laue

## Slide 19: Different techniques
DIffraction
Neutron
Spallation source
T.O.F
Continuous source
X-ray
Monochromatic beam
Laue

## Slide 20: Different techniques
DIffraction
Neutron
Spallation source
T.O.F
Continuous source
X-ray
Monochromatic beam
Laue

## Slide 21: Determination of wavelength
Crystal monochromator (Bragg diffraction)
Sample
Source
Detector
f
qB
Monochromator
(e.g. Si, Ge , Cu, Graphite..)
https://www.mlz-garching.de/englisch/neutron-research/neutron-source.html
Notes: https://slideplayer.com/slide/2401938/

## Slide 22: Dependence of the resolution on 2q
* V could be negative.
There is a minimal FWHM near the angle of the monochromator-take-off.
Why important?
Neutrons
F(Q)
Q
Nuclear
Spin
F(x)
Fmax
Fmax/2
0
q1
q2
FWHM

## Slide 23: Different resolution depending on the beamline
G.4.1 (LLB) l = 2.45 Å
3T2 (LLB) l = 1.25 Å
http://www-llb.cea.fr/
Magnetic structure !!
Crystal structure !!

## Slide 24: Different resolution depending on the wavelength
User guide HRPT

## Slide 25: Different resolution depending on the beamline
l = 1.88 Å
l = 2.45 Å
HRPT (PSI)
DMC (PSI)

## Slide 26: Different techniques
DIffraction
Neutron
Spallation source
T.O.F
Continuous source
X-ray
Monochromatic beam
Laue

## Slide 27: T.O.F diffraction
T.O.F diffraction (angle-dispersive):
use a white beam (neutrons with different wavelengths travel at different speeds)
Instead of varying the scattering angle (fixed angle f),measuring their flight time t over a distance L in order to determine velocity of neutrons (wavelength)
the time-of-flight of neutrons when pulsed beams are applied.
t = 0 is naturally signaled by the start of the pulse.
Sample
Pulsed source
Detector
L1
L2
f
m: Mass of neutron
h: Plank constant
L: Total flying distance (L1+L2)

## Slide 28: T.O.F diffraction
m: Mass of neutron
h: Plank constant
L: Total flying distance (L1+L2)
Cover wide Q-range by different bank detectors.
  Possible to refine crystal and magnetic structure at same time
Data volume is usually huge.
  Requires to combine diffractogram from different bank.
Sample
Pulsed source
Detector
L1
L2
f
Notes: So here basically no geometrical restriction due to the moving detector, principally you can measure up to infinity Q range by turning initiial velocity by modulater and covering the whole range by detector.
This is the biggest advantage,

## Slide 29: T.O.F powder diffraction (Spallation)
Example: GEM data
Resolution function of T.O.F
+ +
Low angle Bank 1
Back scattering Bank 6
Bank 2
Bank 3
Bank 4
90° Bank 5

## Slide 30: Different techniques
DIffraction
Neutron
Spallation source
T.O.F
Continuous source
X-ray
Monochromatic beam
Laue
Single crystal
Powder diffraction
Single crystal
Powder diffraction

## Slide 31: Materials
Bi metal
~cm
~nm
Single crystal
Bi metal
Powder

## Slide 32: Classification of Techniques
Powder
Polycrystal
Monochromatic beam
Variable Angle
Varied by different grains (orientations)
Powder diffraction
  Many small crystallites are randomly oriented.
  Diffraction condition is met at points in 3D reciprocal space.
  Measure in one direction
Single crystal diffraction
  One large crystallite
  Diffraction condition is met at points in 3D reciprocal space.
  Appropriate for larger molecules and unit cells

## Slide 33: Diffraction pattern
Single crystal diffraction pattern
In reciprocal space
a
Powder diffraction pattern
In reciprocal space
Notes: Constructure

## Slide 34: Diffraction pattern
Single crystal diffraction pattern
In reciprocal space
a
Powder diffraction pattern
In reciprocal space
Notes: Constructure

## Slide 35: Diffraction patterns
Diffraction gives the reciprocal point lattice in single crystal
Using powder, the rotation averaging leads to smooth diffraction rings
Position of spots or lines follow to Bragg equation
Debye Scherrer rings
Laue spots

## Slide 36: Laue vs Single crystal diffraction
Single crystal diffraction (Rotation method)
  Monochromatic radiation hits a sample as it is rotated and manipulated to bring different planes into diffraction condition.
  Single crystal diffractometer either 3- or 4- circle goniometers.
  The sample rotates along an axis f
  In order to cover all the diffraction spots in 3D, the goniometer must rotate along axes W and c

## Slide 37: Example: D9
ILL webpage

## Slide 38: Laue vs Single crystal diffraction
Laue method
  The Laue method is mainly used to determine the orientation of large single crystals.
  The Bragg angle is fixed.
  Each set of planes picks out and diffracts the particular wavelength from the white radiation that satisfies the Bragg law for the values of d and q involved.
The Laue method is mainly used to determine the crystal orientation.
  Preparation for the single crystal experiment
  Sample quality check (single? or poly?)
  Required lattice parameters information
  Neutron Laue is useful if you want to align many crystals
  for neutron experiment!
Notes: The radiation is reflected from , or transmitted through a fixed crystal. The diffracted beams form arrays of spots, that lie on curves on the film.

## Slide 39: Example: OrientExpress
ILL webpage

## Slide 40: Powder Diffraction: Constant wavelength
http://www-llb.cea.fr/
Powder diffraction
  A technique used to characterize the crystallographic structure, crystallite (grain) size, preferred orientation in polycrystalline or powdered solid samples.

## Slide 41: Example:D2B
ILL webpage
Notes: The polychromatic beam from the thermal guide H22 is diffracted by the monochromators with a take-off angle of 44.22º towards the sample positions which is 3000mm downbeam.
The sample, a polycrystalline powder, loaded inside a cylinder vanadium can, diffracts the monochromatic incident beam.
The Bragg reflections are mesured by a multi-detector with 1280 cells with a separation of 0.1º, covering the angular range 0.8 to 128.8º. A whole diffraction pattern is thus collected while the detector remains steady.
Note the Radial Oscillating Collimator (ROC) which eliminates the parasitic diffraction beams from sample environment devices.
The recorded neutron diffraction patterns (bottom-left inset) make it possible to study the structure of matter and phase transitions.

## Slide 42: Powder diffraction and the Rietveld refinement

## Slide 43: Before… neutron diffraction!
Good sample – single phase, good crystallinity
  Necessary for structural analysis (complex or novel phases)
Basic characterization
  XRD in the laboratory
  Crystal structure
  Chemical compositions
  Physical properties
Pattern Simulation (very different from XRD one)
Write beamtime proposal (select correct source + instrument)s
Notes: Indexing_powder_diffraction_data_TCH.pdf

## Slide 44: Experiment

## Slide 45: Software list (just a part)
FullProf (ILL, Juan Rodriguez-Carvajal)
Jana2006 (Institute of Physics, Praha, Vaclav Petricek)
GSAS (US, Robert Von Dreele, Brian Toby)
Rietan (NIMS,Japan, Fujio Izumi)
Z-Reitveld (KEK, Japan)
TOPAS (BRUKER)
X’Pert highscore (Panalytical)

## Slide 46: Installation of FullProf
(1) Install Fullprof Suite
(2) Download Exercises -dat

## Slide 47: Installation of VESTA

## Slide 48: Recommendation: Editor
Notepad++ : MS
TextWrangler: Mac

## Slide 49: FullProf package

## Slide 50: How to open the diffraction pattern (Fullprof)
Many European neutron facility formats are covered!

## Slide 51: Step by Step data analysis
Identification of phases
Indexing the Bragg peaks
Space group determination
Structure solution
Structure refinement

## Slide 52: Identification of phases
Identification of know phases
  You know what it is!
  Start with the known structural information!
K. Krishnan et al., J. Alloys Compd. 316, 264–268 (2001).

## Slide 53: Identification of phases
Identification of know phases
  You know what it is!
  Start with the known structural information!
  Novel phase?
  Try Powder pattern-matching by searching the data base.
  It might be known!
  Search the ICSD structural database based on information you have!

## Slide 54: 2.Indexing the Bragg peaks
Software (in Fullprof suite)
ITO [J.W.Visser, J.Appl, Cryst.2 (1969) 89.]
TREOR [P.E.Werner, Z. Krist. 120 (1964) 375.]
DICVOL [D.Louer, J. Appl. Cryst. 18 (1972) 271. A. Boultif,D.Louer, J.Appl. Cryst. 37 (2004)]
Orthorhombic System:
2q positions of reflections
→ Lattice parameters

## Slide 55: 2.Indexing the Bragg peaks
Give the position of Bragg peak position
Give possible crystal system
Give wavelength
RUN!

## Slide 56: 3.Space group determination
Checking the possible space group based on the extension rule!
Try and error refinement using different combination of SG and cell parameter

## Slide 57: Le Bail Fit
Le Bail fit (Profile matching)
Bragg positions (Indexation)
No atomic position information
But SG and lattice constant + Peak shape parameters
Software tries to fit intensity as nice as possible. (Scale is a free parameter.)
2
No structure information
Scale factor: Fixed
Number of atom: 0

## Slide 58: Rietveld refinement
Rietveld refinement
Analysis of Intensities
Structural information
  Atomic form factor
  Position of atoms
  Thermal displacement parameters
  Magnetic moments
This is the standard method to treat powder diffraction data for structure refinement.
Introduced by Hugo Rietveld in 1967, 1969
[H.M. Rietveld, Act Cryst. 22 (1967) 151]
[H.M. Rietveld, J.App.Cryst. 2 (1969) 65]
0

## Slide 59: The calculated profile

## Slide 60: The calculated profile
Calculated
intensity

## Slide 61: The calculated profile
Calculated
intensity
Scale factor

## Slide 62: The calculated profile
Calculated
intensity
Scale factor
Sum over all Bragg peaks

## Slide 63: The calculated profile
Calculated
intensity
Scale factor
Sum over all Bragg peaks
Lorentz factor
Monochromator polarization correction
For neutron

## Slide 64: The calculated profile
Calculated
intensity
Scale factor
Sum over all Bragg peaks
Lorentz factor
Structure factor

## Slide 65: The calculated profile
Calculated
intensity
Scale factor
Sum over all Bragg peaks
Lorentz factor
Structure factor
Profile parameter

## Slide 66: The calculated profile
Calculated
intensity
Scale factor
Sum over all Bragg peaks
Lorentz factor
Structure factor
Profile parameter
Preferred orientation

## Slide 67: The calculated profile
Calculated
intensity
Scale factor
Sum over all Bragg peaks
Lorentz factor
Structure factor
Profile parameter
Preferred orientation
Absorption

## Slide 68: The calculated profile
Calculated
intensity
Scale factor
Sum over all Bragg peaks
Lorentz factor
Structure factor
Profile parameter
Preferred orientation
Absorption
Background

## Slide 69: The calculated profile
Calculated
intensity
Scale factor
Sum over all Bragg peaks
Lorentz factor
Structure factor
Profile parameter
Preferred orientation
Absorption
Background
The parameters in ycalc undergo a least-square refinement to minimize Rwp

## Slide 70: Structure factor with structural parameters
`
u2 :the root mean square displacement of the atom from its average position
The structure factor
B-factor/ Thermal displacement parameter

## Slide 71: Structure factor with structural parameters
The profile function
Gaussian:
Lorentzian:
Gaussian
Lorentzian

## Slide 72: Structure factor with structural parameters
The profile function
pseudo-Voigt:
Fullprof: Npr = 5
Strain-dependent
Instrumental parameters (Sample independent)
Size-dependent
The Thompson-Cox-Hastings pseudo-Voigt
Fullprof: Npr = 7

## Slide 73: FullProf: Powder diffraction analysis
Data file
.PCR file: Input file (Fullprof reads lines)
Fix : 0
Vary :1
Input
Output
Experimental set-up
Refinement parameters
Experimental set-up 2
Excluded regions
Number of refined parameter
Background
Main control codes line for the phase
Space group
Atomic
parameter
(option) Bond-Valence or distance and angles calculations
Scale factor
Profile parameter
Cell parameter

## Slide 74: Let’s try together
  MgAl2O4
  Data from Fullprof website
Space Group: F d -3 m
Atomic position
Tetrahedral A-positions (Mg,Al) 8a (1/8,1/8,1/8)
Octahedral B-positions (Mg,Al) 16d (1/2,1/2,1/2)
Oxygen positions (O) 32e (x,x,x) x = 0.26
Unit cell : a = 8 Å
1 Mg Mg1 0.00000 0.00000 0.00000 1.000 1.000 8a -43m
2 Al Al1 0.62500 0.62500 0.62500 1.000 1.000 16d .-3m
3 O O1 0.38730 0.38730 0.38730 1.000 1.000 32e .3m
Neutron powder diffraction
T = 300K
3T2 (LLB) (Data format: INS=1)
l = 1.227 Å
Profile parameters function NPR=7
MgO impurity
Space Group: F m -3 m
Atomic position
Mg positions (Mg) 4a (0,0,0)
Oxygen positions (O) 4b (1/2, 1/2, 1/2)
Unit cell : a = 4.22 Å

## Slide 75: Steps of the refinement
Refinement in several steps
  Scale factor
  Background
  Lattice parameters and zero shift
  Atomic positions
  Thermal parameter
  Occupational parameters (if necessary )
  Profile parameters
You can refine structure (these parameters) using diffraction data!

## Slide 76: FullProf files
Data file
.PCR file: Input file
.OUT file
.SUM file
.CIF file - VESTA
.HKL file

## Slide 77: Difficulties
More parameters More difficult!
High background
Peak broadening
  Anisotropic
  Asymmetric shape
Too large or too small crystallites
Absorption
More than single phase (impurity)
Low symmetry..!

## Slide 78: Now you try!: LaMnO3
Crystal structure determination of LaMnO3: 300K, 573K, 798K
  Data from Fullprof website
Space Group: P b n m
Atomic position
La 4c (0, 0.05, 0.25)
Mn 4a (1/2 0 0)
O1 4c (0, 0.49, 0.25)
O2 8d (0.7, 0.3, 0.04)
Unit cell : a = 5.5 Å, b = 5.7 Å, c = 7.7 Å
Neutron powder diffraction
T = 300K, 573K and 798K
3T2 (LLB) (Data format: INS=6)
l = 1.227 Å
Profile parameters function NPR=7
A signature of phase transition above 798K, but this time we will fit whole temperature pattern using same structure (Pbnm).
Biso: start from 1.00
Zero: 0.00
Refine profile parameter: Y only start from 0.00
Mission (1) Find unit cell (using DICVOL)
(2) Le Bail Fit
(3) Rietveld refinement starting from structure above
(4) Plot unit cell parameters, bond distances and thermal displacement parameters
(5) Visualize the refined structure using VESTA