## Slide 1
Quasi-Elastic Neutron Scattering (QENS) …
… what can high energy resolution neutron spectroscopy tell us?
Mark Telling
mark.telling@stfc.ac.uk

## Slide 2
QENS : Learning Goals
Upon completion of this module, and subsequent
guided analysis of real experimental QENS data, you will be able to:
  describe the energy, time and length scales accessible using the QENS method
  visualise the neutron scattering cross section and the ensuing benefit of isotope labelling
  differentiate between coherent / incoherent scattering
  distinguish between different QENS instrument classes
  extract diffusion coefficients, activation energies, transition temperatures and geometries of motion

## Slide 3
So … why investigate dynamics ?
“by understanding the microscopic dynamics we can tune a materials bulk properties”

## Slide 4
QENS : Quasi-Elastic Neutron Scattering
  well established neutron method
  Quasi-Elastic Neutron Scattering, M. Bée, 1988, ISBN-10: 0852743718
Tailored to measure low-energy (< 2 meV) excitations
  atomic or molecular excitations ‘diffusive’ in origin
Experimental dataset : peak of intensity, I, and width, G
  model the peak’s breadth as a function of T, P, composition to extract parameters linked to macromolecular movement
  intensity can exhibit marked angular variation which can give information about the geometry of the motion observed
So … what is QENS ?

## Slide 5
QENS: spatial and temporal landscape

## Slide 6
Neutron Source
Detector 1, Intensity(1,Es)
QENS and the Time of Flight (ToF) technique
velocity selector
Eincident
Escattered
distance, L1
distance, L2
q2
q1
Detector 2,
Intensity(2,Es)

## Slide 7
Chart: 
Neutron Source
Detector 1, Intensity(1,Es)
Detected Intensity
Ei = Es : elastic scattering
velocity selector
Eincident
Escattered
distance, L1
distance, L2
q2
q1
Detected Intensity
Lets heat things up …
time of arrival at detector
time of arrival at detector
Detector 2,
Intensity(2,Es)

## Slide 8
Detected Intensity
DE
Neutron Source
Detector 1, Intensity(1,DE)
Detected Intensity
Ei = Es : elastic scattering
velocity selector
Eincident
Escattered
distance, L1
distance, L2
q2
q1
Lets heat things up …
DE (energy transferred) = 0
mobile material
Signal from
immobile material
Detector 2,
Intensity(2,DE)
FFT
neutron instruments can see motions that occur on the pico-second to nano-second time scale
Chart: 

## Slide 9
Detected Intensity
DE
Neutron Source
Detected Intensity
Ei = Es : elastic scattering
velocity selector
Eincident
Escattered
distance, L1
distance, L2
q2
q1
sample relaxation time, t
1
0
Lets heat things up …
DE (energy transferred) = 0
mobile material
Signal from
immobile material
FFT
neutron instruments can see motions that occur on the pico-second to nano-second time scale
Chart: 
Detector 1, Intensity(1,DE)
Detector 2,
Intensity(2,DE)

## Slide 10
Scattering Angle, q
is related to the momentum transfer
vector, Q, by…
Qki=kf = 4(-1)sin(q/2)
i
…which, when we relate this to Braggs law
is inversely proportional
to the length scale being observed
q  Q  1/length scale
Note!
i
Neutron Source
Detector 1, Intensity(Q1,DE)
QENS and the Time of Flight (ToF) technique
velocity selector
Eincident
Escattered
distance, L1
distance, L2
q2
q1
Detector 2,
Intensity(Q2,DE)
Light,
ultra low x-rays
SANS, SAXS
Wide angle, intermediate angle
Increasing scattering Angle, q or Q

## Slide 11
Neutron Source
Information extracted …
velocity selector
Eincident
Escattered
distance, L2
q2
q1
Dynamics
Geometry
I(Q,t)
Ielastic
Inon-el
1
0
distance, L1
sample relaxation time, t
neutron instruments see motion(s) that occur on the pico-second to nano-second time scale
Detector 1, Intensity(Q1,DE)
Detector 2,
Intensity(Q2,DE)

## Slide 12
q, |Q|
DE = 0
I
The Scattering Function : S(Q,w)
We don’t just have one detector collecting data, but many. The intensity and/or breath of the peaks measured in different detectors can vary.
Now, the signal measured in any detector is a measurement of the double differential cross section
“…the probability that a neutron of incident energy Ei is scattered with into a solid angle element dW about the direction W and with a change of energy between E=ħw=Ef – Ei and ħ(w+dw)”
Ultimately, scientists want to measure ‘something’ directly related to the sample alone which he/she can fit/model …
Scattering Function: S(Q,w)
… it so happens that this ‘probability’ is dependent on how the neutron interacts with a sample; and this interaction in Q and E is unique to the specific macromolecule studied

## Slide 13
In reality …
DE = 0
In reality …
Intrinsic broadening around the DE = 0 positions is due to ‘instrument’ effects.
Defines the sensitivity, or resolution, of the instrument
= instrument contribution

## Slide 14
No!
While, for x-rays, the scattering strength is proportional to Z
The power to scatter neutrons varies randomly across the periodic table
Amplitude of scattered wave is dependent on the neutron – nucleus interaction, b (known as the scattering length)
b effectively dictates the strength of the neutron – nucleus interaction
In practice, we speak of the neutron-nucleus interaction in terms of area
Scattering cross section:  = 4b 2
This effective area related to the probability that there will be a interaction
Do all atoms scatter neutrons equally?

## Slide 15
No!
While, for x-rays, the scattering strength is proportional to Z
The power to scatter neutrons varies randomly across the periodic table
Do all atoms scatter neutrons equally?

## Slide 16
Element | Scattering xs | Absorption xs
1H | 82.03 | 0.3326
2H | 7.64 | 0.000519
Li | 1.37 | 70.5
C | 5.551 | 0.0035
O | 4.232 | 0.00019
Na | 3.28 | 0.53
S | 1.026 | 0.53
Cross-sections in units of area known as the barn (b) = 10-24 cm2
The scattering power of hydrogen …

## Slide 17
Element | Scattering xs | Absorption xs
1H | 82.03 | 0.3326
2H | 7.64 | 0.000519
Li | 1.37 | 70.5
C | 5.551 | 0.0035
O | 4.232 | 0.00019
Na | 3.28 | 0.53
S | 1.026 | 0.53
Cross-sections in units of area known as the barn (b) = 10-24 cm2
The scattering power of hydrogen …

## Slide 18
Element | Scattering xs | Absorption xs
1H | 82.03 | 0.3326
2H | 7.64 | 0.000519
7Li | 1.4 | 0.04
C | 5.551 | 0.0035
O | 4.232 | 0.00019
Na | 3.28 | 0.53
S | 1.026 | 0.53
Cross-sections in units of area known as the barn (b) = 10-24 cm2
The scattering power of hydrogen …

## Slide 19
hydrogen
carbon
oxygen
Why is this advantageous ?

## Slide 20
Selective deuteration
Element | Scatter | Abs
1H | 82.03 | 0.3326
2H | 7.64 | 0.000519
Li | 1.37 | 70.5
C | 5.551 | 0.0035
O | 4.232 | 0.00019
Na | 3.28 | 0.53
S | 1.026 | 0.53
total measured neutron intensity is dominated by signal from the H atoms
hydrogen
carbon
oxygen

## Slide 21
Selective deuteration
Detected Intensity
Element | Scatter | Abs
1H | 82.03 | 0.3326
2H | 7.64 | 0.000519
Li | 1.37 | 70.5
C | 5.551 | 0.0035
O | 4.232 | 0.00019
Na | 3.28 | 0.53
S | 1.026 | 0.53
D
D
D
D
D
D
D
D
D
D
D
D
D
D
D
D
D
D
deuterium
carbon
oxygen
spectral contribution from H atom position is greatly reduced
D

## Slide 22
At Bragg condition - constructive
Away from Bragg condition - destructive
d
extra distance bottom wave has to travel compared to top wave to remain IN PHASE = 2d(sin) (aka Bragg’s Law)
 (d)


Coherent and Incoherent Scattering …
Perfect crystal with i nuclei all of scattering length, b

## Slide 23
At Bragg condition
Away from Bragg condition
d
Coherent and Incoherent Scattering …
d
extra distance bottom wave has to travel compared to top wave to remain IN PHASE = 2d(sin) (aka Bragg’s Law)


Perfect crystal with i nuclei, most with b but also some isotopes with b’

## Slide 24
d
Coherent and Incoherent Scattering …
d
extra distance bottom wave has to travel compared to top wave to remain IN PHASE = 2d(sin) (aka Bragg’s Law)


Perfect crystal with i nuclei, most with b but also some isotopes with b’
Crystalline Polyethylene (Y. Takahashi)

## Slide 25
So how do these two types modify the detected intensity …
Coherent
Coherent vs Incoherent Scattering …
In-coherent
… because we now have a system of i species with a mean scattering length, <bi>, and a root mean deviation from this mean, √(<bi2>-<bi>2), our total scattering cross section, s = 4b2, can be written …
… such that our measured intensity …
… comprised of both coherent and incoherent signals
Van Hove L. Correlations in Space and Time and Born Approximation Scattering Phys Rev 1954; 95: 249-262.

## Slide 26
So what do these two types of scattering tell us …
Coherent
describes correlations between different atoms at different times
Coherent vs Incoherent Scattering …
In-coherent
describes correlations between
the position of a single atom at
different times
Van Hove L. Correlations in Space and Time and Born Approximation Scattering Phys Rev 1954; 95: 249-262.

## Slide 27
So … what information can we extract ?

## Slide 28
Line Width Analysis : activation energies, D

## Slide 29
Geometry : Elastic Incoherent Structure Factor

## Slide 30
Elastic Window Scans : transitions and ‘rigidity’
To determine transition temperatures
  plot neutron intensity at the DE = 0 position vs. temperature
  deviations from linearity suggest a transition
To determine the mean squared displacement (msd) parameter, <r2>, from Elastic Window plots
  Plot neutron intensity (@ DE=0) vs. temperature vs. Q
  Fit:
=
Tg

## Slide 31
Energy Transfer, DE = Eincident – Efinal
Therefore, to determine DE we need to define Ei OR Ef
QENS Instrumentation

## Slide 32
Energy Transfer, DE = Eincident – Efinal
http://www.ill.eu/instruments-support/instruments-groups/instruments/in5
Instrumentation : direct geometry
defines Ei
probes: mostly local motion(s)
t : pico-second
length scale : 1 - 30 Å
mostly incoherent signal
measure : S(Q,w)
signal in detector

## Slide 33
Energy Transfer, DE = Eincident – Efinal
http://www.ill.eu/instruments-support/instruments-groups/instruments/in16
Instrumentation : indirect geometry
defines Ef
probes: mostly local motion(s)
t : pico- to nano-second
length scale : 1 - 30 Å
mostly incoherent signal
measure : S(Q,w)
signal in detector

## Slide 34
broadband
examines: mostly collective motion(s)
t : nano-second
length scale : comparable to SANS
mostly coherent signal
measure : I(Q,t)
http://www.ill.eu/instruments-support/instruments-groups/instruments/in11
Instrumentation : neutron spin echo
However, we can also use a spin polarised beam …
signal in detector

## Slide 35
Putting it all together …
Notes: Origin of the term “scattering cross-section”
The scattering cross-section expresses the probability that a particle will be scattered as it transverses a given thickness of matter dx. Classically,  = d2 is a target area that each molecule presents to the oncoming particles. This target area is a cross-section of the region within which a collision can take place, as viewed along the direction of motion of the beam.
see also Appendix 1

## Slide 36
Paul Ehrlich and the ‘magic bullet’ concept
‘a drug which can be transported to a specific organ within the body and released at a controlled rate without affecting surrounding organisms’
Notes: Having been responsible for a neutron instrument dedicated to problems at the physics – life science interface I have had the privilege to work on many bio-physics problems from the point of view of neutron scattering. For example
The behaviour of cytoplasmic water
Bio-protective characteristics of trehalose
Controlled assembly in water of large proteins into high performance silk fibres
36

## Slide 37
drug delivery system
  hydrogel-based micro spheres
retains water up to 99 % its weight
responds to environmental stimuli
proposed application
  contain bioactive drug in solution in gel pores
basic drug delivery requirements
  biocompatibility, good solvent diffusivity
key to development is understanding gel behaviour
  characterise the polymer mobility vs cross links, chemical and physical nature of cross links, hydrophobicity, investigate how gel behaviour intertwined with movement of confined water
By cross linking poly (vinyl alcohol) chains a
‘polymer sponge’ is formed
‘magic bullets’ and plastic sponges
Notes: Origin of the term “scattering cross-section”
The scattering cross-section expresses the probability that a particle will be scattered as it transverses a given thickness of matter dx. Classically,  = d2 is a target area that each molecule presents to the oncoming particles. This target area is a cross-section of the region within which a collision can take place, as viewed along the direction of motion of the beam.
see also Appendix 1

## Slide 38
initial interest
  characterise the raw hydrogel material
focus
  rationalise how structural features influence diffusive properties of solvent
material to be used
  poly (vinyl alcohol) (PVA)
why PVA ?
a) bio-compatible
b) used in surgery as thread for stitches
c) thermally stable and acid tolerant
By cross linking poly (vinyl alcohol) chains a
‘polymer sponge’ is formed
‘magic bullets’ and plastic sponges
Notes: Origin of the term “scattering cross-section”
The scattering cross-section expresses the probability that a particle will be scattered as it transverses a given thickness of matter dx. Classically,  = d2 is a target area that each molecule presents to the oncoming particles. This target area is a cross-section of the region within which a collision can take place, as viewed along the direction of motion of the beam.
see also Appendix 1

## Slide 39
Hydrogel and H2O
‘magic bullets’ and plastic sponges
T = 10 oC 25 oC 30 oC
Notes: Origin of the term “scattering cross-section”
The scattering cross-section expresses the probability that a particle will be scattered as it transverses a given thickness of matter dx. Classically,  = d2 is a target area that each molecule presents to the oncoming particles. This target area is a cross-section of the region within which a collision can take place, as viewed along the direction of motion of the beam.
see also Appendix 1

## Slide 40
Hydrogel and H2O
‘magic bullets’ and plastic sponges
T = 10 oC 25 oC 30 oC
Notes: Origin of the term “scattering cross-section”
The scattering cross-section expresses the probability that a particle will be scattered as it transverses a given thickness of matter dx. Classically,  = d2 is a target area that each molecule presents to the oncoming particles. This target area is a cross-section of the region within which a collision can take place, as viewed along the direction of motion of the beam.
see also Appendix 1

## Slide 41
Hydrogel and H2O
‘magic bullets’ and plastic sponges
Notes: Origin of the term “scattering cross-section”
The scattering cross-section expresses the probability that a particle will be scattered as it transverses a given thickness of matter dx. Classically,  = d2 is a target area that each molecule presents to the oncoming particles. This target area is a cross-section of the region within which a collision can take place, as viewed along the direction of motion of the beam.
see also Appendix 1

## Slide 42
Hydrogel and H2O
‘magic bullets’ and plastic sponges
Notes: Origin of the term “scattering cross-section”
The scattering cross-section expresses the probability that a particle will be scattered as it transverses a given thickness of matter dx. Classically,  = d2 is a target area that each molecule presents to the oncoming particles. This target area is a cross-section of the region within which a collision can take place, as viewed along the direction of motion of the beam.
see also Appendix 1

## Slide 43
Hydrogel and H2O
Peak is made up of 3 components
polymer relaxation, p
water diffusive motion, d
water rotational motion, r
‘magic bullets’ and plastic sponges
Notes: Origin of the term “scattering cross-section”
The scattering cross-section expresses the probability that a particle will be scattered as it transverses a given thickness of matter dx. Classically,  = d2 is a target area that each molecule presents to the oncoming particles. This target area is a cross-section of the region within which a collision can take place, as viewed along the direction of motion of the beam.
see also Appendix 1

## Slide 44
Hydrogel and H2O vs. Hydrogel and D2O
Polymer Segmental Relaxation
a) water (H2O) b) deuterium (D2O) confined in a PVA based hydrogel
‘magic bullets’ and plastic sponges
Notes: Origin of the term “scattering cross-section”
The scattering cross-section expresses the probability that a particle will be scattered as it transverses a given thickness of matter dx. Classically,  = d2 is a target area that each molecule presents to the oncoming particles. This target area is a cross-section of the region within which a collision can take place, as viewed along the direction of motion of the beam.
see also Appendix 1

## Slide 45
Water dynamics
Fickian Diffusion Model
Random, Jump Diffusion
D = diffusion coefficient
o = residence time
‘magic bullets’ and plastic sponges
Notes: Origin of the term “scattering cross-section”
The scattering cross-section expresses the probability that a particle will be scattered as it transverses a given thickness of matter dx. Classically,  = d2 is a target area that each molecule presents to the oncoming particles. This target area is a cross-section of the region within which a collision can take place, as viewed along the direction of motion of the beam.
see also Appendix 1

## Slide 46
Neutrons have helped us understand …
… how we can tune diffusivity
cross link dependent diffusion, Dwater
… the nature of the water-polymer interaction
governed by hydrogen-bonding
… that diffusion is not continuous (Fick's Law)
… that the diffusion rate is Arrhenius :
Dwater = Doexp(-Ea/RT)
… that T = 290K, Dwater is less than Dbulk water
super cooling effect
Bulk Water
0.05
0.02
0.1
‘magic bullets’ and plastic sponges
Notes: Origin of the term “scattering cross-section”
The scattering cross-section expresses the probability that a particle will be scattered as it transverses a given thickness of matter dx. Classically,  = d2 is a target area that each molecule presents to the oncoming particles. This target area is a cross-section of the region within which a collision can take place, as viewed along the direction of motion of the beam.
see also Appendix 1

## Slide 47
Tutorial : Guided Data Reduction and Analysis
  Using a guided ‘workbook’ approach the ideas presented in this lecture will be enforced by following standard raw data reduction and analysis procedures to:
  explore translational diffusion characteristics (water)
  explore rotational diffusion characteristics (protein)
  familiarise yourself issues faced when analysing QENS data
Analysis will be performed using the Mantid package
  the software platform adopted at ESS, ISIS, ILL and SNS
  workbook based on version 4.0.0
On the USB stick you should find:
  workbook
  all experimental data sets required
  supplementary data files
  further reading
Notes: Having been responsible for a neutron instrument dedicated to problems at the physics – life science interface I have had the privilege to work on many bio-physics problems from the point of view of neutron scattering. For example
The behaviour of cytoplasmic water
Bio-protective characteristics of trehalose
Controlled assembly in water of large proteins into high performance silk fibres
47

## Slide 48
e-mail: mark.telling@stfc.ac.uk
Thank you!