## Slide 1: Inelastic scattering by phonons
Gediminas Simutis :: Paul Scherrer Institute
Nordic Neutron School, Tartu, October 29th, 2021

## Slide 2
Neutron scattering
Neutrons see where the atoms are and what they do
1994 Clifford G. Shull Bertram N. Brockhouse

## Slide 3
Overview
Introduction
What are phonons?
INS cross section
Practical aspects
Examples:
  Soft-mode transition in SrTiO3
  Kohn anomalies
  Phonons in superconductors
  Phonons in quantum magnets

## Slide 4
Lattice excitations
Phonons are important for understanding:
Specific heat
Structural and electronic instabilities
Electron coupling in superconductors
…

## Slide 5
Molecular vibrations
O2 molecule, E = 0.25 eV, ‘stretching mode’
No momentum dependence
A simple example

## Slide 6
A simple example
A chain of atoms connected by springs
a

## Slide 7
A simple example
A chain of atoms connected by springs
a

## Slide 8
A simple example
A chain of atoms connected by springs
Small movements around equilibrium
a
un
un-1
un+1

## Slide 9
A simple example
A chain of atoms connected by springs
Small movements around equilibrium
a
un
un-1
un+1

## Slide 10
A simple example
A chain of atoms connected by springs
Small movements around equilibrium
a
un
un-1
un+1

## Slide 11
A simple example
A chain of atoms connected by springs
Small movements around equilibrium
a
un
un-1
un+1
Using Newton’s 2nd law, equate to

## Slide 12
A simple example
A chain of atoms connected by springs
Small movements around equilibrium
a
un
un-1
un+1
Using Newton’s 2nd law, equate to
Now taking the plane wave ansatz

## Slide 13
with
rearrange and use Euler
+ double angle identity

## Slide 14
Different Atoms
Two different atoms per unit cell
a

## Slide 15
Different Atoms
Two different atoms per unit cell
a
u2n
u2n-1
u2n+1
M1 M2

## Slide 16
Different Atoms
Two different atoms per unit cell
a
u2n
u2n-1
u2n+1
M1 M2
Two differential equation and two trial solutions for the different atoms
Substitution provides:

## Slide 17
Different Atoms

## Slide 18
Different Atoms

## Slide 19
Different Atoms

## Slide 20
Different Atoms

## Slide 21
Different Atoms

## Slide 22
Different Atoms

## Slide 23
Different Atoms
Homogeneous equations -> to solve, set determinant to zero
If invertible
X = A^-1 b,
But b = 0,
So only trivial

## Slide 24
Different Atoms
Homogeneous equations -> to solve, set determinant to zero

## Slide 25
Different Atoms
Homogeneous equations -> to solve, set determinant to zero

## Slide 26
Different Atoms
Homogeneous equations -> to solve, set determinant to zero
Limits

## Slide 27
Different Atoms
Homogeneous equations -> to solve, set determinant to zero
Limits

## Slide 28
Measured phonons
Monoatomic (Neon) Diatomic (NaCl)
Raunio et al., 1969
Endoh et al., 1975
6.5 and 23.7 K (melting point, 24.6 K)
1 THz = 4 meV
VdW

## Slide 29
Measured phonons
Monoatomic (Al) Diatomic (SrO)
Rieder et al., 1975
Stedman, Nilsson, 1965

## Slide 30
Measured phonons
Monoatomic Diatomic
Rieder et al., 1975
Stedman, Nilsson, 1965
Total number of normal modes = 3N,
Where N = # of atoms in unit cell
3 of them acoustic, other – optical
Speed of sound = dw/dq

## Slide 31
A note on quantum derivation
Operators!

## Slide 32
A note on quantum derivation
Operators!
Harmonic oscillator
Substitute by raising and lowering
Rearrange for x and p and sub
___
number operator

## Slide 33
A note on quantum derivation
One dimension
After a similar procedure – q !
Three dimensions
q and polarization p
Operators!
Harmonic oscillator
Substitute by raising and lowering
Rearrange for x and p and sub
___
number operator

## Slide 34
How to measure, cf Raman/IR
Neutron spectroscopy
cross section spectrum (q-dep)
Raman spectroscopy
cross section spectrum (q~0 only)
BZ ~ 1/a
qmax ~ 2k ~ 1/l

## Slide 35
How to measure, cf Raman/IR
Neutron spectroscopy
cross section spectrum (q-dep)
Raman spectroscopy
cross section spectrum (q~0 only)
IXS:
Baron,
arXiv:1504.01098
~ 10 keV

## Slide 36
Three-axis spectroscopy

## Slide 37
Time-of-flight spectroscopy

## Slide 38
Scattering cross section

## Slide 39
Scattering cross section
Prefactors Transition probability E-conservation
(Fermi Golden Rule)

## Slide 40
Scattering cross section
Prefactors Transition probability E-conservation
(Fermi Golden Rule)
After manipulations arrive at a general function:
Property of the sample
For detailed derivation, see for example Ch2 of Squires

## Slide 41
Phonon cross section
The general form can be calculated for specific cases.
Example: 1-phonon scattering

## Slide 42
Phonon cross section
The general form can be calculated for specific cases.
Example: 1-phonon scattering

## Slide 43
Phonon cross section
The general form can be calculated for specific cases.
Example: 1-phonon scattering
Phonon emission
Phonon absorption

## Slide 44
Phonon cross section
The general form can be calculated for specific cases.
Example: 1-phonon scattering
Scales as
And 1/

## Slide 45
Phonon cross section
The general form can be calculated for specific cases.
Example: 1-phonon scattering
Debye-Waller factor
Population factors
(reduction of intensity: phonons relevant also for elastic scattering)
For a cubic system

## Slide 46
Effect of temperature
Detailed balance principle
Your sample is also a thermometer!

## Slide 47
Effect of temperature
Detailed balance

## Slide 48
Effect of temperature
Detailed balance
Ba8Ge38Zn8
Koza et al., (2010)

## Slide 49
Incoherent Scattering
Total scattering cross section
So far we have been discussing only the coherent case
Pair correlation function
“probability G(r,t) of finding an atom at (r,t) given that there is another
atom at r = 0 at time t = 0”
Incoherent scattering – self correlation function
“probability G(r,t) of finding the same atom at (r,t) given that the same atom was at r = 0 at time t = 0”
In practice, the relative importance is nucleus dependent
https://www.nist.gov/ncnr/neutron-scattering-lengths-list

## Slide 50
Incoherent Scattering
DOS of phonons
Can be used to obtain absolute cross-section

## Slide 51
Incoherent Scattering
DOS of phonons
Can be used to obtain absolute cross-section

## Slide 52
Incoherent Scattering
DOS of phonons
Can be used to obtain Accurate comparison with models absolute cross-section
GS et al., (2017)

## Slide 53
Incoherent Scattering
DOS of phonons
The cross-section is the same for powder samples at high q
(Incoherent approximation)
low q: high q:
small part of BZ all BZ
coherence effects incoherent
This is how DOS of phonons is usually obtained
Taken from ISIS n-school

## Slide 54
Phonon widths
Brockhouse et al., (1962): Phonons in Pb
Peaks in Energy dependence have finite widths
Resolution + phonon lifetime
Axe and Shirane (1973)

## Slide 55
Phonon widths
Brockhouse et al., (1962): Phonons in Pb
Peaks in Energy dependence have finite widths
Resolution + phonon lifetime
Phonons and superconductivity
Nb3Sn
Phonons with energy less than the SC gap have fewer decay channels (electron-hole decay suppressed)
Axe and Shirane (1973)

## Slide 56
Examples

## Slide 57
  Soft-mode transition in SrTiO3
  Kohn anomalies
  Phonons in superconductors
  Phonons in quantum magnets
Examples

## Slide 58
  Soft-mode transition in SrTiO3
  Kohn anomalies
  Phonons in superconductors
  Phonons in quantum magnets
Examples

## Slide 59
Phases and Phase Transitions

## Slide 60
Phases and Phase Transitions
Dagotto 2005

## Slide 61
Phases and Phase Transitions
How do they take place?
Dagotto 2005

## Slide 62
Structural transition in SrTiO3
Cubic perovskite at Tetragonal at room temperature low temperature
Shirane, Yamada 1969

## Slide 63
Structural transition in SrTiO3
Cubic perovskite at Tetragonal at room temperature low temperature
Shirane, Yamada 1969

## Slide 64
Structural transition in SrTiO3
Cubic perovskite at Tetragonal at room temperature low temperature
Shirane, Yamada 1969
~ 108 K

## Slide 65
Structural transition in SrTiO3
Cubic perovskite at Tetragonal at room temperature low temperature
Shirane, Yamada 1969
~ 108 K

## Slide 66
Structural transition in SrTiO3
Step 1 – structure
New Bragg peaks appear at LT

## Slide 67
Structural transition in SrTiO3
Step 1 – structure
New Bragg peaks appear at LT

## Slide 68
Structural transition in SrTiO3
Step 2 – dynamics: phonon spectrum

## Slide 69
Structural transition in SrTiO3
Step 2 – dynamics: phonon spectrum

## Slide 70
Structural transition in SrTiO3
Step 3 – The soft phonon

## Slide 71
Structural transition in SrTiO3
Step 3 – The soft phonon

## Slide 72
Structural transition in SrTiO3
Step 3 – The soft phonon

## Slide 73
Structural transition in SrTiO3
Step 3 – The soft phonon
Energy goes to 0 as T approaches TC
The structure is unstable to this phonon

## Slide 74
Structural transition in SrTiO3
Step 3 – The soft phonon
Triply degenerate
2 + 1 degeneracy

## Slide 75
Summary of SrTiO3 story
Neutrons could see:
structure change
and
the excitations that are responsible for it
Frozen phonon mechanism
Change of degeneracies between
different structures.
The triply degenerate soft mode is split by
the distortion into a singlet mode with the
rotation axis parallel to the static distortion
and a doublet mode with the rotation axes
perpendicular to the distortion

## Slide 76
More of SrTiO3 story
Albeit an archetypical transition, it shows unusual critical indexes:
Critical fluctuations
Experiments observe two energy scales and two length scales
(See for example Cowley 1996)

## Slide 77
  Soft-mode transition in SrTiO3
  Kohn anomalies
  Phonons in superconductors
  Phonons in quantum magnets
Examples

## Slide 78
How about the electrons ?
Previous example – electrons irrelevant.
Is it always the case?

## Slide 79
How about the electrons ?
Previous example – electrons irrelevant.
(often think about Born-Oppenheimer)
Is it always the case?

## Slide 80
How about the electrons ?
Previous example – electrons irrelevant.
(often think about Born-Oppenheimer)
Is it always the case? Let’s start with electrons this time. Fermi sea to be precise

## Slide 81
How about the electrons ?
Previous example – electrons irrelevant.
(often think about Born-Oppenheimer)
Is it always the case? Let’s start with electrons this time. Fermi sea to be precise

## Slide 82
Instabilities at Fermi surface
Charge density wave (CDW)

## Slide 83
Lindhard’s functions
c
In 1-D – divergence
Higher D – no (sphere)

## Slide 84
Lindhard’s functions
However, even at D > 1
CDW can occur in the case of nesting: shape of fermi surface!
c
In 1-D – divergence
Higher D – no (sphere)
1D nesting 2D – no 2D - partial

## Slide 85
Lindhard’s functions
However, even at D > 1
CDW can occur in the case of nesting: shape of fermi surface!
c
In 1-D – divergence
Higher D – no (sphere)
1D nesting 2D – no 2D - partial
G. Gruener, Density Waves in Solids, 1994

## Slide 86
E-P coupling and Kohn anomaly
G. Gruener, Density Waves in Solids, 1994
Electrons ‘dress’ nuclei
(like viscous fluid for a solid)
Frozen phonon for 1D

## Slide 87
E-P coupling and Kohn anomaly
G. Gruener, Density Waves in Solids, 1994
Electrons ‘dress’ nuclei
(like viscous fluid for a solid)
Frozen phonon for 1D

## Slide 88
E-P coupling and Kohn anomaly
G. Gruener, Density Waves in Solids, 1994
Electrons ‘dress’ nuclei
(like viscous fluid for a solid)
Frozen phonon for 1D

## Slide 89
E-P coupling and Kohn anomaly
G. Gruener, Density Waves in Solids, 1994
Electrons ‘dress’ nuclei
(like viscous fluid for a solid)
Frozen phonon for 1D
A chain of Pt
1D overlap of dz² orbs

## Slide 90
E-P coupling and Kohn anomaly
G. Gruener, Density Waves in Solids, 1994
Electrons ‘dress’ nuclei
(like viscous fluid for a solid)
Frozen phonon for 1D
Comes et al., 1975

## Slide 91
  Soft-mode transition in SrTiO3
  Kohn anomalies
  Phonons in superconductors
  Phonons in quantum magnets
Examples

## Slide 92
Superconductivity
Kammerling-Onnes 1911
Unique He Liquifier

## Slide 93
Superconductivity – BCS theory
Phonon couples the two electrons into a pair

## Slide 94
Superconductivity – BCS theory
Phonon couples the two electrons into a pair
Debye frequency
DOS
e-e attraction

## Slide 95
Superconductivity – BCS theory
Phonon couples the two electrons into a pair
TC related to the phonons: McMillan’s formula
Debye frequency
e-ph interaction coulomb repulsion
~
~
Need metals with very light elements

## Slide 96
Superconductivity – BCS theory
~
~
~

## Slide 97
Isotope effect
Drozdov et al., 2015
Szczęśniak et al., 2018

## Slide 98
Isotope effect
Drozdov et al., 2015
Szczęśniak et al., 2018
See Physics Today (2016)
DOI:10.1063/PT.3.3220

## Slide 99
Room temperature?
LaH10±x
Somayazulu et al., 2018
https://arxiv.org/abs/1808.07695
Physics Today article
DOI:10.1063/PT.6.1.20180823b

## Slide 100
Room temperature?
LaH10±x
Somayazulu et al., 2018
https://arxiv.org/abs/1808.07695
Now PRL 122, 027001 (2019)
Physics Today article
DOI:10.1063/PT.6.1.20180823b
+ Physics viewpoint article:
https://physics.aps.org/articles/v12/1

## Slide 101
More practical materials
MgB2 example – “unconventionally conventional”
DFT + neutron scattering to identify the phonon and estimate coupling
Incoherent approximation used for neutron scattering !
Osborn 2001 also:
TC ~ 39 K
https://www.ncnr.nist.gov/staff/taner/mgb2/

## Slide 102
More practical materials
MgB2 example – “unconventionally conventional”
Very large l (0.9), because of particular phonon.
DFT + neutron scattering to identify the phonon and estimate coupling
Incoherent approximation used for neutron scattering !
Osborn 2001 also:
TC ~ 39 K
https://www.ncnr.nist.gov/staff/taner/mgb2/

## Slide 103
More practical materials
MgB2 example – “unconventionally conventional”
Very large l (0.9), because of particular phonon.
DFT + neutron scattering to identify the phonon and estimate coupling
Incoherent approximation used for neutron scattering !
Osborn 2001 also:
TC ~ 39 K
https://www.ncnr.nist.gov/staff/taner/mgb2/

## Slide 104
Unconventional Superconductors
Christianson et al., 2008
Iron-based superconductors
TC = 28 K
LaFeAsO1-xFx

## Slide 105
Unconventional Superconductors
Christianson et al., 2008
Iron-based superconductors
TC = 28 K
LaFeAsO1-xFx
Small l (0.21)
Resulting TC < 1

## Slide 106
  Soft-mode transition in SrTiO3
  Kohn anomalies
  Phonons in superconductors
  Phonons in quantum magnets
Examples

## Slide 107
Quantum magnets

## Slide 108
Quantum magnets

## Slide 109
Quantum magnets
Mourigal et al.,
NPhys 9, 435–441 (2013)

## Slide 110
T/J
1/S, 1/z (1/D), frustration
Playground of quantum magnets
Bethe (1931)
Néel (1932)
Landau (1933)
Anderson (1952)
Mermin and Wagner (1966)
Chakravarty et al., (1989)
Chubukov et al., (1994)
Balents (2010)

## Slide 111
Quantum magnets
frustrated 2D
Shastry-Sutherland lattice
realized by SrCu2(BO3)2
Pressure-driven transitions
Zayed et al., 2017
Interesting phases
But difficult to characterize

## Slide 112
Quantum magnets
frustrated 2D
Shastry-Sutherland lattice
realized by SrCu2(BO3)2
Pressure-driven transitions
Zayed et al., 2017
Interesting phases
But difficult to characterize
Can phonons help us to understand the intermediate phase?

## Slide 113
Quantum magnets
development of pair spin correlations at low temperatures
-> magnetic contribution to the rigidity of the corresponding bond
Very difficult to disentangle the exact nature – can still provide info about PTs
Bettler, GS et al., 2017

## Slide 114
Quantum magnets
development of pair spin correlations at low temperatures
-> magnetic contribution to the rigidity of the corresponding bond

## Slide 115
Quantum magnets
development of pair spin correlations at low temperatures
-> magnetic contribution to the rigidity of the corresponding bond
In SCBO, very well-defined special phonon
“pantograph mode”
Energy ~

## Slide 116
Quantum magnets
Bettler et al., 2019 arXiv:1907.09316; Now PR Research 2, 012010(R) (2020)
FM
AFM

## Slide 117
Quantum magnets
Can phonons be used to control the magnetism then ?
* Not directly related to the Raman experiment discussed above, because selection rules are different.
Using Intense 1 ps THz pulses to excite phonons
-> Magnetophononics resonant spin excitation (lives 10s of ps)

## Slide 118
Quantum magnets
Can phonons be used to control the magnetism then ?
The best is yet to come.. Fine and targeted control

## Slide 119
Phonons hold many secrets to the behaviour of numerous interesting and potentially useful materials.
Neutron scattering is often the appropriate key to unlock them.
Enjoy your time while doing it.
Thank you for your attention

## Slide 120
Extra slides

## Slide 121
Incoherent scattering

## Slide 122
Incoherent scattering

## Slide 123
Incoherent scattering

## Slide 124
Incoherent scattering

## Slide 125
Correlation functions

## Slide 126
Correlation functions

## Slide 127
Correlation functions
Intermediate function
Correlation
function
Scattering
function
measure calculate
Van Hove, 1954

## Slide 128
Correlation functions

## Slide 129
Incoherent scattering

## Slide 130
Incoherent scattering

## Slide 134
QM treatment of phonons
Sum
Diff
Plug
For lattice:

## Slide 135
QM treatment of phonons
Sum
Diff
Plug
For lattice:

## Slide 136
QM treatment of phonons
Sum
Diff
Plug
For lattice:

## Slide 141
Correlation functions
What is the meaning of G

## Slide 142
Spin density wave

## Slide 143
Kohn anomalies also in Chromium !
Fawcett - RMP

## Slide 144
Specific heat

## Slide 154
Reduction of intensity – phonons relevant even for elastic scattering
For a cubic system
DW factor

## Slide 155
Superconductivity – BCS theory
Phonon couples the two electrons into a pair
TC related to the phonons: McMillan’s formula
DOS